석공 D 201-2010

	대한석탄공사 물품규격	석공 D 201
	(KOCOAL ARTICLE STANDARD)	제정 1987. 1
		개정 2006.12
	와 이 어 로 프 ( WIRE ROPE )	개정 2010.12
Specification
HS NO. Description Q‘ty
7312,10,2099 Head Wire Rope 4 Reels
1．Quotation
A. Quotation is requested for four (4) reels head wire ropes as described in this
specification.
B. Four (4) reels each 1,080 meters to be used as hoisting ropes on 3.04 meters
diameter friction type hoist in the coal mine.
2．Technical Specification
A. The wire rope provided under this specification shall comply with the applicable
provisions of EN12385-6, DIN21258 & TAS 6
B. Wire rope description
1) Length : Four (4) reels each 1,080 meters long
2) Diameter : 38 mm
3) Construction : 6 × 31
warrington - seale
Preformed
round strand
Heavy galvanized
4) Core : polyamid fibre core

석공 D 201-2010

5) Lay : Ordinary

Two (2) reels - left hand lay(zS).

Two (2) reels - right hand lay(sZ).

6) Nominal tensile strength of wires : 1,770 N/㎟

7) Calculated breaking load : minimum 1,070 KN

8) Weight : 5.66 ～5.72 Kg/m

9) Lubrication : According to DIN 21258 (Nyrosten N 113)

C. Rope reel

The ropes shall be all individually wind on fabricated robust steel reel.

(* Reference : attached drawing, Reel Drum 1,480×900×1,600)

3．General Condition

Bidder shall include a full description of the wire rope being offered.

The successful bidder shall furnish a inspection report(test certificate of wire rope)

being supplied.

Specification

HS   NO.                         Description                               Q‘ty

7312,10,2099                      Head Wire Rope                          5 Reels

1．Quotation

A. Quotation is requested for five (5) reels head wire ropes as described in this

specification.

B. Five (5) reels each 1,220 meters to be used as hoisting ropes on 5.5 meters

diameter friction type hoist in the coal mine.

2． Technical Specification

석공 D 201-2010

A. The wire rope provided under this specification shall comply with the applicable

provisions of EN12385-6, DIN21258 & TAS 6

B. Wire rope description

1) Length : Five (5) reels each 1,220 meters long

2) Diameter : 48 mm

3) Construction : 6 × 36

warrington - seale

Preformed

round strand

Heavy galvanized

4) Core : polyamid fibre core

5) Lay : Ordinary

Two (2) reels - left hand lay(zS).

Two (3) reels - right hand lay(sZ).

6) Nominal tensile strength of wires : 1,770 N/㎟

7) Calculated breaking load : Minimum 1,530 KN

8) Weight : 8.83 kg/m (Max 9.0 kg/m)

9) Lubrication : According to DIN 21258 (Nyrosten N 113)

C. Rope reel

The ropes shall be all individually wind on fabricated robust steel reel.

(* Reference : attached drawing, Reel Drum 1,550×1,200×2,500)

3．General Condition

Bidder shall include a full description of the wire rope being offered.

The successful bidder shall furnish a inspection report(test certificate of wire rope)

being supplied.

석공 D 201-2010

Specification

HS   NO.                         Description                               Q‘ty

7312,10,2099                        Tail Rope                              3 Reels

1．Quotation

A. Quotation is requested for P․E coated balance wire ropes as described in this

specification.

B. Each reel of 1,100meters length to be used as Balancing ropes under 3.04meters

diameter friction type hoist in the coal mine.

2． Technical Specification

A. The wire rope provided under this specification shall comply with the applicable

provisions of B.S of DIN.

B. Wire rope description

1) Length : Each reel 1,100 meters length

2) Diameter : 45 mm (Finished Dia)

3) Construction : 34 × 9

Round type strand

Cushion polyethylene coated rope

Preformed

heavy galvanized.

4) Core : IWRC

5) Lay and direction of lay : Non rotating Right hand lang's lay(sZ)

6) Nominal tensile strength of wires : 1,080 N/㎟

7) Calculated breaking load : Minimum 823 KN

8) Weight : 7.63 kg/m

9) Lubrication : According to DIN 21258 (Nyrosten N 113)

석공 D 201-2010

C. Rope reel

The ropes shall be all individually wind on fabricated steel reel.

(* Reference : attached drawing, Reel Drum 1,480×1,000×1,780)

3. General Condition

Bidder shall include a full description of the wire rope being offered.

The successful bidder shall furnish a inspection report(test certificate of wire rope)

being supplied.

Specification

HS   NO.                          Description                               Q‘ty

7312,10,2099                         Tail Rope                              3 Reels

1．Quotation

A. Quotation is requested for P․E coated balance wire ropes as described in this

specification.

B. Each reel of 1,130 meters length to be used as balancing ropes under 5.5 meters

diameter friction type hoist in the coal mine.

2． Technical Specification

A. The wire rope provided under this specification shall comply with the applicable

provisions of B.S of DIN.

B. Wire rope description

1) Length : Each reel 1,130 meters length

2) Diameter : 65 mm (Finished Dia)

3) Construction : 34 × 19

Round type strand

석공 D 201-2010

Preformed

Cushion Polyethylene coated rope

Non - rotating

heavy galvanized.

4) Core : IWRC

5) Lay and direction of lay : Right regular lay(sZ)

6) Nominal tensile strength of wires : 1,080 N/㎟

7) Calculated breaking load : Minimum 1,670 KN

8) Weight : 15.0 kg/m

9) Lubrication : According to DIN 21258 (Nyrosten N 113)

C. Rope reel

The ropes shall be all individually wind on fabricated steel reel.

(* Reference : attached drawing, Reel Drum 1,550×1,500×3,200)

3. General Condition

Bidder shall include a full description of the wire rope being offered.

The successful bidder shall furnish a inspection report(test certificate of wire rope)

being supplied.

석공 D 201-2010

석공 D 202-2010

	대한석탄공사 물품규격				석공 D 202
	(KOCOAL ARTICLE STANDARD)				제정 1987. 1
					개정 2006.12
	파 이 프 ( P I P E )				개정 2010.12
1．적용범위：이 규격은 KS D 3507 및 KS D 3564 배관용 탄소 강관의 빅토릭 조인트
식의 연결용 파이프에 대하여 규정한다.
2．제조방법 : KS 배관용 탄소강관 압착식으로 한다.
3．품 질
4．시 험				KS D 3507 및 3567에 의한다
5．검 사
6．표 시

석공 D 203-2010

	대한석탄공사 물품규격	석공 B 203
	(KOCOAL ARTICLE STANDARD)	제정 1987. 1
		개정 2010.12
	관 이 음 쇠 ( PIPE JOIN IRON )
1．나사식 가단 주철제 관 이음쇠 : KS표시품 (KS B 1531)
2．나사식 배수관 이 음 쇠 : KS 의거품 (KS B 1532에 의거)
3．나사식 강관제 관 이음쇠 : KS 의거품 (KS B 1533에 의거)
4．플랜지식 관 이음쇠 : KS 의거품

석공 D 204-2010

	대한석탄공사 물품규격	석공 D 204
	(KOCOAL ARTICLE STANDARD)	제정 1987. 1
		개정 2010.12
	밸 브 ( VALVE )
1．적용범위 : 이 규격은 Pipe 접속용 밸브에 대하여 규정한다.
2．종 류 : 2.1 청동 5 kg/㎠ 나사식 글러브 밸브 : KS 표시품 (KS B 2301)
2.2 청동 5 kg/㎠ 나사식 게이트 밸브 : KS 표시품 (KS B 2303)
2.3 청동 10 kg/㎠ 볼 밸브 : KS 표시품 (KS B 2308)
※ 부도 2 : 첨부 도면으로 한다.
2.4 청동 10 kg/㎠ 볼밸브 1종 글러브 밸브 : KS 표시품 (KS B 2311)
2.5 청동 10 kg/㎠ 볼밸브 1종 앵글 밸브 : KS 표시품 (KS B 2312)
2.6 청동 10 kg/㎠ 볼밸브 1종 게이트 밸브 : KS 표시품 (KS B 2313)
2.7 주철 10 kg/㎠ 플랜지형 1종 글러브 밸브 : KS 표시품 (KS B 2351)
2.8 주철 10kg/㎠ 플랜지형 1종 안나사 게이트밸브 : KS 표시품 (KS B 2353)
2.9 주강 10 kg/㎠ 플랜지형 1종 글러브 밸브 : KS 표시품 (KS B 2361의거)
2.10 주강 20 kg/㎠ 플랜지형 1종 글러브 밸브 : KS 표시품 (KS B 2365)
2.11 주강 20 kg/㎠ 플랜지형 1종 바깥나사 게이트 밸브 : KS 표시품 (KS B 2367)
2.12 주강 20 kg/㎠ 플랜지형 1종 스윙 체크 밸브 : KS 표시품 (KS B 2368)

석공 D 205-2010

			대한석탄공사 물품규격								석공 D 205
			(KOCOAL ARTICLE STANDARD)								제정 1987. 1
											개정 2010.12
			빅 토 릭 조 인 트 ( VICTAULIC JOINT )
1．적용범위：이 규격은 파이프 접속용으로 사용되는 빅토릭 조인트(Victaulic Joint)에
대하여 규정한다.
( 단, 이 기준의 운용에 있어 별도의 정함이 있을 때는 그 정하는 바에 따
른다).
2．종 류 : 빅토릭 조인트는 □표1□과 같이 적용 강관의 호칭구분에 따라 4종으로
구분한다.
		표 1.
		A (m/m)			100		150	200		250
		B (inch)			4		6	8		10
3．호 칭 : 빅토릭 조인트는 체결용 볼트 너트 및 기밀용 고무링을 포함하여 1조로
하며 적용 강관의 호칭구분 및 제조 재질에 따른다. 호칭은 □표1□의 A
또는 B 어느 것을 칭하여도 무방하며 필요에 따라 숫자의 뒤에 첨가 구
분한다. (예) 호칭 200 A 빅토릭 조인트 제조 재료가
3.1 탄소 주강인 경우 : 200A - SC 또는 8″A - SC
3.2 구상 흑연주철의 경우 : 150A GCD 40 또는 6″B GCD 40
4．문자삽입 : 제품의 상단표면에 부각체로 호칭구분 및 제조자명 또는 약호를 삽입한다
5．제조재질 : 제조재질은 다음표의 재질 또는 동등 이상의 재질로 한다.
	표 2
	호 칭					재 질			비 고
	A			B
	100			4		GCD 40			KSD 4302 1종
	150			6		〃			〃

석공 D 205-2010

6．제조방법

6.1 주조품은 용선로, 전기로, 반사로, 기타 적당한 용해로에서 용해하고 주방 상태에서

흑연을 구상화시키기 위한 적당한 처리를 하여 제조한다.

6.2 주강품은 로내에서 각부 균일하게 가열하여 어닐링(Annealing) 노오말징(Normal-

izing) 또는 노오말징 후 템퍼링(Tempering) 중의 한 방법에 의하여 열처리한다.

6.3 주조품은 어닐링(Annealing) 기타의 열처리를 한다.

7．모양 및 치수 : 모양 및 제 치수는 부도에 따른다.

8．품   질

8.1 주조품의 품질은 균일하며 면은 원활하고 해로운 흠 균열 및 기포가 없어야 한다.

8.2 치운친 살 등의 결함이 없어야 한다.

8.3 표면은 매끈하여야 하며 표면 거칠기가 KS B 0161의 200S 이하를 원칙으로 한다.

단 주강품의 가공면은 35S 이하로 한다.

8.4 각 치수는 균일하여 호환성 있게 제작할 것.

9．도    장 : 필요에 따라 요구시 외부 표면에 적당한 방청 처리한다. (콜탈 등)

10．치수허용차 : 도면 및 부표에 명시된 치수허용차 외는 KS B 0418(주강품 보통 허용

차) 정밀급 및 KS B 0411(주조 가공치수차) 정밀급에 준한다.

11．시    험

11.1 공시재는 사형에 구조하고 그것을 대표하는 제품과 동일로에서 열처리 한 것을

원칙으로 한다.

11.2 시험은 KS B 0802 (금속재료 인장시험 방법) 및 KS B 0804 (금속재료 굽힘 시

험방법)에 따른다.

11.3 수압시험은 모형단관에 부품 삽입조립 후 수압을 가하여 17.5 kg/㎠ 수압상태에서

각 3분씩 보존 시험하여 이상 없을 것.

석공 D 205-2010

12．검    사

12.1 겉모양 및 치수 검사는 매 제품 실시함을 원칙으로 하되 품질 및 허용치 수치를

기준으로 판정한다.

12.2 인장시험 및 굴곡시험은 KS에 의거 판정한다.

12.3 수압 검사는 규정 압력 상태에서 규정 시간 보존하였을 때 균열 및 누수 등 기타

결함 유무를 확인 판정한다.

12.4 제 시험 결과 시험의 일부가 기준과 상이할 때는 관련 규정이 정하는 바에 따라

재시험할 수 있다.

13．기    타

13.1 빅토릭조인트용 고무링을 별도 제조기준에 의한다.

13.2 빅토릭조인트 체결용 볼트 너트는 부도의 구조에 의하여 품질은 흑피급으로 한다

석공 D 206-2010

	대한석탄공사 물품규격	석공 D 206
(KOCOAL ARTICLE STANDARD)	제정 1987. 1
	개정 2010.12
	G - I 빔 ( G - I BEAM )
1．적용범위：이 규격은 갱내 지보 재료로 사용되는 I -형강(G-I Beam)에 대하여 규정
한다.
2．제조방법：1) 강재는 평로, 선로 또는 전기로에 의한 강괴로부터 제조한다.
2) 강재는 사상(Finishing)이 양호하고 품질이 균일하며 사용상 유해한 결
함이 있어서는 안 된다.
3．화학성분 : 강재의 화학성분은 래들(Ladle) 분석치로서 표1에 따른다.
	표 1.
	구 분	C	Mn	P	S	비 고
	G - I 100	-	-	0.05 이하	0.05 이하	G-I 130 공용
4．기계적 성질 : 강재의 인장강도, 항복점, 연신률 및 굴곡은 표2에 따른다. 다만 굴곡의
경우 그 바깥쪽에 균열이 생겨서는 안 된다.
	표 1
	항목 종류	인 장 시 험	굴곡시험	비 고
항복점kg/㎟	인장강도kg/㎟	신 률 %	굴곡각도(°)
	G - I 100	30 이상	50 이상	20 이상	180	G - I 130 공용
5．겉모양, 형상, 치수, 무게 및 그 허용차
5.1 I형강의 겉모양, 형상, 치수, 무게와 그 허용차는 다음과 따른다.
	표 3
	구분 종류	단 면 촌 법	단면적 ㎠
A	B	t1	t2	r1	r2
	G - I 100	100	80	9	12.5	13	4	26.4	20.7	403	80.5	3.91	1.75	80.7	20.1
	G - I 130	130	100	12	17	16	7	44.6	35.0	1,130	211	5.05	2.18	175	42.3

석공 D 206-2010

단, 관성 모멘트, 회전반경, 단면 계수를 참고로 표시하며 규격의 일부는 아님.
5.2 허용치
	표 4
	구 분			허 용 차
	폭, 길이 ( A, B )			± 2 mm
	복부두께 ( t1 )			± 0.8 mm
	길이 ( 7mm 이하 )			＋ 40 mm － 0.0 mm
	길이 ( 7mm 이상 )			7 mm 초과 1 m당 5 mm 가산
6．시 험 7．검 사 8．표 시		｝	KS D3503에 의한다 (일반구조용 압연강재)
9．기 타 : 부재 곡률 적용 시험을 행함에 있어 곡률 반경은 실제 사용 곡률 반경에
1/2로 한다.

석공 D 207-2010

				대한석탄공사 물품규격											석공 D 207
				(KOCOAL ARTICLE STANDARD)											제정 1987. 1
															개정 2010.12
				레일 이음매판 ( FISH PLATE )
1．적용범위：이 규격은 Rail 연결용에 사용되는 레일 이음매판( Fish Plate )에 대하여
규정 한다.
2．종 류 : 종류는 표1에 의한다.
			표 1
			품 명						구 분
			이 음 매 판						30 kg 레 일 용
			〃						22 kg 〃
			〃						20 kg 〃
			〃						15 kg 〃
			〃						9 kg 〃
3．사용재료 : KS D3503 (일반 구조용 압연강재) 2종 이상의 것을 사용 할 것.
4．화학성분 : 화학성분은 □표2□에 의한다.
	표 2
	품 명						종 류	기 호			C	Mn		P		S
	레일연결용 이음매판 (Fish Plate)						2 종	SB 41			―	―		0.05 이하		0.05 이하
5．기계적 성질 : 인장강도, 신률, 곡률은 표3에 의한다. 다만 굴곡의 경우는 그 바깥쪽
에 균열이 생겨서는 안 된다.
		표 3
		종 류			기 호	인장강도(kg/㎟)				신 률(%)			굴곡시험
		2 종			SB 41	41 ～ 52				17 이상			180°에서 양호

석공 D 207-2010

6．품질, 형상, 치수 및 그 허용차

6.1 두께 : KS D3500(열간 압연강판 및 강대의 형상 치수와 그 허용차)에 의한다.

6.2 우리 공사가 제시하는 도면 또는 샘플에 의거 제작하되 표면은 매끈하고 균열, 터짐

등 유해한 점이 없어야 하며 다듬질은 양호하여야 한다.

6.3 모든 굴곡부분은 굴곡이 균일하여야 한다.

석공 D 208-2010

			대한석탄공사 물품규격										석공 D 208
			(KOCOAL ARTICLE STANDARD)										제정 1987. 1
													개정 2003.12
			이 음 매 판										개정 2010.12
1．적용범위：이 규격은 G․I Beam 연결용으로 사용하는 이음매판에 대하여 규정한다.
2．종 류 : 종류는 다음에 의한다.
2.1 이음매판 1) 100 G․I Beam 용
2) 130 G․I Beam 용
3．사용재료 : KS D3503(일반 구조용 압연강재) 2종 이상의 것을 사용할 것.
4．화학성분 : 화학성분은 표1에 의한다.
	표 1
	종 류			기 호		C		Mn		P		S
	2 종			SS 41		―		―		0.05 이하		0.05 이하
5．기계적 성질 : 인장강도, 신률, 곡률은 표2에 의한다. 다만, 굴곡의 경우는 그 바깥쪽
에 균열이 생겨서는 안된다.
		표 2
		종 류			기 호		인장강도(kg/㎟)		신률 (%)		굴곡시험
		2 종			SS 41		41 ～ 52		17 이상		180°에서 양호
6．품질, 치수 및 그 허용차
1) 두께 : KS D 3500 (열간 압연강판 및 강대의 형상 치수와 그 허용차)에 의한다.
2) 우리 공사가 제시하는 별첨도면에 의거 단조용 가열로에서 가열하여 조직에 손상이
없도록 제작하되 표면은 매끈하고 균열, 터짐 등 유해한점이 없어야 하며 다듬질은
양호하게 제작하여야 한다.
3) 모든 굴곡 부분은 굴곡이 균일하여야 한다.

석공 D 208-2003

석공 D 209-2010

						대한석탄공사 물품규격									석공 D 209
						(KOCOAL ARTICLE STANDARD)									제정 1987. 1
															개정 2003.12
						대 못 ( S P I K E )									개정 2010.12
1．적용범위：이 규격은 경레일에 사용되는 대못(Spike)에 대하여 규정한다.
2．종 류 : 종류는 표1에 의한다.
			표 1
			품 명						구 분
			대 못						30 Kg 레 일 용
			〃						22 Kg 〃
			〃						15 Kg 〃
3．사용재료 : KS D 3503 (일반 구조용 압연강재) 2종 이상의 것을 사용 할 것.
4．화학성분 : 화학성분은 □표2□에 의한다.
	표 2
	종 류			기 호				C		Mn		P		S
	2 종			SS 41				―		―		0.05 이하		0.05 이하
5．기계적 성질 : 인장강도, 신률, 곡률은 표3에 의한다.
		표 3
		종 류			기 호		인장강도(Kg/㎟)				신 률(%)		굴곡시험
		2 종			SS 41		41 ～ 52				17 이상		180°에서 양호
6．품질, 형상, 치수 및 그 허용차
6.1 우리 공사가 제시하는 도면 또는 샘플에 의거 제작하되 표면은 매끈하고 균열, 터짐
등 유해한 점이 없어야 하고 굴곡부분이 없이 곧아야 한다.
6.2 형상은 도면 또는 샘플에 의하되 정사각형의 단면으로 각 모서리의 각은 90°를 유
지하고 날카로우며 끝부분은 뭉툭하면 안 된다.

석공 D 209-2010

7. 치수
단위 : m/m
치수 규격	A	B	C	D	E	F	G	H	I	비 고
30kg 用	16	130	39	34	17	10	19	30	15
22kg 用	12	115	34	28.5	13	8	17.5	22	15
15kg 用	12	100	34	28.5	13	8	17.5	22	14
허용공차	+ 0.5 - 0.0	± 20	+ 0.5 - 0.0	+ 0.5 - 0.0						공통적용

석공 D 301-2000

			대한석탄공사 물품규격														석공 D 301
			(KOCOAL ARTICLE STANDARD)														제정 1987. 1
																	개정 2010.12
			화이트 메탈 ( Babbit )
1．적용범위：이 규격은 화이트 메탈(Babbit)에 대하여 규정한다.
2．모양 치수 및 무게 : 주괴는 취급하기 편리한 모양, 치수로 하고 특히 지정이 없는
한 무게는 10 kg 이하로 한다.
3．화학성분 : 화학성분은 표1에 따른다.
	표 1
	종 별	기 호		Sn		Sb		Cu	As	불 순 물								비고
										Pb	Fe	Zn	Al	Bi	As	Cu
	1 종	WM1		잔부		5.0 ～ 7.0		5.0 ～ 7.0	―	0.05 이하	0.08 이하	0.01 이하	0.01 이하	0.08 이하	0.10 이하	―
	2 종	WM2		〃		8.0 ～ 10.0		8.0 ～ 10.0	―	〃	〃	〃	〃	〃	〃	―
4．시험 및 검사					｝
							KS D 6003에 의함
5．표 시

석공 D 302-2000

				대한석탄공사 물품규격							석공 D 302
				(KOCOAL ARTICLE STANDARD)							제정 1987. 1
											개정 2010.12
				청 동 지 금 (Bronze Base Metal)
1．적용범위：이 규격은 주물용의 청동지금에 대하여 규정한다.
2．품 질
2.1 지금은 품질이 균일하고 표면이 깨끗하여야 하며, 용재(Slag)나 기타 다른 물질이
함유되어서는 안 된다.
2.2 화학성분은 표1에 따른다.
	표 1
	종 류	기 호				화 학 성 분						색 별
						Cu	Sn	Zn	Pb	불순물
	2 종	BrC2				86.0～90.0	7.0 ～ 9.0	3.0 ～ 5.0	―	1.0 이하		적 색
	3 종	BrC3				86.5～89.5	9.0 ～11.0	1.0 ～ 3.0	―	1.0 이하		백 색
3．시 험			｝
4．검 사					KS D 6003에 의함
5．표 시